## Slide 1: Microbial fuel cells that have been performed in my lab
김성현

## Slide 2: Development of Microbial Fuel Cells Using Proteus vulgaris
Bull. Korean Chem. Soc. 2000, 21, 44

## Slide 3: Effect of Initial Carbon Sources on the Performance of Microbial Fuel Cells Containing Proteus vulgaris
Biotechnology and Bioengineering. 2000, 70, 119.

## Slide 4: Optimization of the performance of microbial fuel cells containing alkalophilic Bacillus sp.
J. Microbial Biotechnol. 2001, 11, 863.

## Slide 5: Effect of initial carbon sources on the electrochemical detection of glucose by Gluconobacter oxydans
Bioelectrochemistry 57 (2002) 173 – 178
Amperometric detection of glucose

## Slide 6: Dynamic Behaviors of Redox Mediators within the Hydrophobic Layers as an Important Factor for Effective Microbial Fuel Cell Operation
Bull. Korean Chem. Soc. 2003, Vol. 24, No. 4 437
Quenching experiments
Fo/F = KSV [Q] + 1

## Slide 7: Membrane Fluidity Sensoring Microbial Fuel Cell
Bioelectrochemistry 59 (2003) 121 – 127
Temperature shock
25 oC
46 oC

## Slide 8: Construction of Microbial Fuel Cells Using Thermophilic Microorganisms, Bacillus Licheniformis and Bacillus thermoglucosidasius
Bull. Korean Chem. Soc. 2004, 25, 813.

## Slide 9: Development of bipolar plate stack for microbial fuel cells.
Bull. Korean Chem. Soc. 2006, 27, 281

## Slide 10: Effect of initial carbon sources on the performance of a microbial fuel cell containing environmental microorganism Micrococcus luteus
Bull.Korean Chem. Soc. 2007, 28, 1591.

## Slide 11: Polypyrrole-coated reticulated vitreous carbon as anode in microbial fuel cell for higher energy output.
Bull. Korean Chem. Soc. 2008, 29, 1344

## Slide 12: Improved performance of a microbial fuel cell with polypyrrole/carbon black composite coated carbon paper anodes
Bull.Korean Chem. Soc. 2008, 29, 1344
Nyquist plot for the plain carbon paper and Ppy/CBcoated carbon paper. Semi-circle parts were fitted to obtain RΩ and Rct.
Power density plot of an MFC with different anodes, Ppy/CB (■) and electrodeposited Ppy anode (●). Electrodeposition of Ppy

## Slide 13: Use of Carbon Nanoparticles for Bacteria Immobilization in Microbial Fuel Cells for High Power Output
Journal of The Electrochemical Society, 2009, 156, B1238.

## Slide 14: Polypyrrole-modified RVC anode in a mediator-type MFC by pure culture
Polypyrrole
Microbe: P. vulgaris
Mediator: methylene Blue
Bull. Korean Chem. Soc. 29 (2008) 168-172

## Slide 15: Polypyrrole/CB composite modified carbon paper anode in a mediator-type MFC
A
B
A: Bare carbon paper
B: CB coated carbon paper
C: Ppy/CB-coated carbon paper
B
Bull. Korean Chem. Soc. 29 (2008) 1344-1348
Microbe: P. vulgaris
Mediator: thionin
Nyquist plots for the plain carbon paper and Ppy/CB-coated carbon paper.

## Slide 16: Polyaniline/Carbon composite modified carbon cloth anode in a single chamber MFC-mixed culture
Carbon cloth
PANI/C-coated carbon cloth
Bull. Korean Chem. Soc. 28 (2015) 2170-2173

## Slide 17: Polyaniline nanofiber-coated macroporous RVC anode for high performance MFCs
SEM images of (a) RVC macrospores, (b) after PANInf modification, and after PANInf modification and heat treatment at 750 oC.
a
b
c
X-ray photoelectron spectra (a) Survey scan for RVC, RVC-PANI & RVC-PANI-HT. (b) De-convulated N1s peaks of RVC-PANI and (c ) Deconvulated N1s peaks for RVC-PANI-HT

## Slide 18
RVC-PANI interior
RVC-PANI exterior
RVC exterior
RVC interior
RVC-PANI-HT exterior
RVC-PANI-HT interior
Biofilm formation on the exterior and interior of RVC
Schematic presentation of typical microbial fuel cell set up

## Slide 19
Charging-discharging curves
CVs at the turn-over conditions
CVs at the substrate depletion conditions
Polarization curves RVC (◇) RVC-PANI (○) RVC-PANI-HT (▷) and corresponding power density curves. MFCs run in 1g/L acetate.

## Slide 20: Electricity generation from non- electroactive bacteria
Biosens. Bioelectron. 27 (2011) 106-112

## Slide 21: Use of Osmium Redox Polymer

## Slide 22: MFC Performance

## Slide 23: Conducting polymers as cathode modifiers for oxygen reduction
Cathode is also important!
O2 + 4H+ + 4e-  2H2O
Trends in oxygen reduction activity plotted as a function of the oxygen binding energy.
J. Phys. Chem. B, 108 (2004) 17886–17892

## Slide 24: Development of non-noble metal oxygen reduction catalysts for air cathodes
Materials
  1. Polyaniline nanofiber/Carbon composite
  2. Polyaniline/Carbon composite/FePc
  3. Multi-walled carbon nanotubes (MWCNT)
  p-MWCNT (pristine)
  a-MWCNT (NH2-functionalized)
  c-MWCNT (COOH-functionalized)
  4. Iron phthalocyanine (FePc)
    MWCNT-supported FePc
  5. Carbon/Cobalt oxide/CoPc

## Slide 25: Polyaniline/C composite air-cathode in a single-chamber microbial fuel cell
Voltage-time curve in a start-up period in 0.1 M PBS buffer under 1 kΩ external load. Substrate =1 g/L glucose.
Repetitive charging-discharging cycle of an MFC with PANI/C air cathode in 0.1 M PBS buffer under 1k Ω external load. Susbtrate=1 g/L glucose.

## Slide 26: Polyaniline/C/FePc as air-cathode in a single-chamber microbial fuel cell
J. Power Sources 196 (2011) 1103.
Cyclic voltammetric characterizations of PANI/C and PANI/C/FePc at a scan rate of 100mV/s (A), CVs of PANI/C/FePc with different scan rates (B), and peak current dependence on scan rates

## Slide 27
CV (A) and LSV of various electrodes for the oxygen reduction at scan rate of 100 mV/s (B) and 1 mV/s (C)

## Slide 28: Polyaniline nanofiber as an ORR catalyst Characterization
SEM (left) and TEM (right) images of synthesized polyaniline nanofiber.
UV/vis spectra of polyaniline nanofiber as prepared (a) and after treating in 0.2 M NH4OH (b).
J. Electrochem. Soc. 159 (2012) B497-B501

## Slide 29: XPS characterization of polyaniline nanofiber and voltage generation in start-up period
N1s XPS spectra for pristine polyaniline nanofiber (A) and polyaniline nanofiber/C (B)
Voltage generation at start-up stage of an MFC with polyaniline nanofiber (●) and polyaniline nanofiber/C (●).

## Slide 30
A: Plot of power density vs current density for PANInf (●), PANInf/C (●), and carbon black (▲) cathode.
B: Individual electrode potential measured with respect to SCE as a function of current density.
% Coulombic efficiency for PANInf/C (a) and Pt/C (b) cathodes.
Effect of the amount of PANInf/C

## Slide 31: Comparison of material costs
Cathode material | Price(g/$) | Power density (mW/m2) | Power per cost of cathode material (mW/$)
Polyaniline/C Pt/C Polyaniline/C/FePc Polyaniline/C/CoPc FePc/C | 3.392 29.38 3.392+7.35 3.392+9.74 0.0718+7.35 | 381.4 575.6 630.5 534.9 336.6 | 7.78 0.55 4.11 2.85 3.17

## Slide 32: MWCNT and MWCNT-supported iron(ІІ) phthalocyanine based oxygen reduction catalysts as cathode in a single-chamber microbial fuel cell
Raman spectra for plain MWCNT (black), COOH-functionalized MWCNT (red), and NH2-functionalized MWCNT (blue).
FETEM images of a-MWCNT (A) and a-MWCNT/FePc (B) samples at different magnifications
Biores. Tech. 102 (2011) 5849-5854

## Slide 33: Electrochemical characterization and voltage output by MWCNT and MWCNT/FePc
CVs of GC, a-MWCNT and a-MWCNT/FePc-coated GC in pH 7 PBS at 10 mV/s.
Voltage output with various MWCNT/FePc and C/FePc coated cloth cathodes at 550ohm using 1 g/L glucose as fuel.

## Slide 34: Power generation with various cathodes
1) Synthetic wastewater - glucose
2) Real wastewater from a sewage treatment plant
Biores. Tech. 102 (2011) 5849-5854

## Slide 35
Cathode | Power density mW/m2(glucose) | Power density mW/m2(wastewater) | CE/%a | COD removalb
Carbon black p-MWCNT c-MWCNT a-MWCNT | 94 146 211 249 | - 47 79 104 | 15 16 20 20 | - 83.5% 82.2% 85.0%
Cathode | Power density mW/m2(glucose) | Power density mW/m2(wastewater) | CE/%a | COD removalb
Carbon/FePc p-MWCNT/FePc c-MWCNT/FePc a-MWCNT/FePc Pt/C | 337 450 521 601 576 | 114 138 181 259 - | 21 21 23 24 25 | - 88.5% 90.2% 91.0% -
Table 1. Summary of MWCNTs cathode performance
Table 2. Summary of MWCNTs/FePc cathode performance
a 1000ohm glucose as fuel b 1000ohm wastewater as fuel
a 550ohm glucose as fuel b 550ohm wastewater as fuel

## Slide 36: Cobalt oxide Nano Particles + Cobalt Phthalocyanine on Carbon
Heating to 110 ℃ then to 400 ℃
C/CoOx
Co(NO3)2·6H2O
Vulkan XC72
CoPc dissolved in chloroform
C/CoOx/CoPc
Applied to the electrode
XRD pattern for C-CoOx (black) and C-CoOx-CoPc (red)
RSC Adv. 4 (2014) 44065-44072

## Slide 37: Characterization by XPS and TEM
A
B
C
XPS spectra for C-CoOx-CPc (A) and C-CoPc (B)
TEM images of synthesized C-CoOx (A), C-CoPc (B), and C-CoOx-CoPc (C)

## Slide 38: Cyclic voltammetry and Tafel plot
(Left) CVs of C-CoPc (black), Co-CoOx (red), and C-CoOx-CoPc (blue) under N2-saturated (thin lines) and O2-saturated (thick lines) at 5 mVs-1.
(Right) Tafel plots for C-CoPc (black), Co-CoOx (red), and C-CoOx-CoPc (blue) in low overpotential region constructed from CV

## Slide 39: Rotating Ring-Disk Electrode Experiments
RRDE experiments
Disk: C/CoOx/CoPc-modified; Ring: Glassy carbon
Condition: O2-saturated, 1600 rpm
Scan rate = 5 mv/s
Disk potential scanned; Ering = 1.2 V vs. SCE
C/CoOx/CoPc
GC ring
Teflon body

## Slide 40: Number of transferred electrons and % hydrogen peroxide yield
Plots of the number of electrons transferred (left) and the percent yield of hydrogen peroxide (right) during the oxygen reduction as a function of potential. All the measurements were done in pH 7 PBS buffer
N : collection efficiency

## Slide 41: Power density curves and individual potential monitoring
(Left) Plot of power density vs. current density for MFCs with different cathodes.
Carbon power, C-CoOx, C-CoPc, C-CoOx-CoPc and C-Pt.
(Right) Individual electrode potential measured with respect to SCE as a function of current density for each cathode material at 5 mgcm-2.

## Slide 42: Effect of C/CoOx/CoPc amount on the power density and long-term operation
Effect of the amount of C-CoOx-CoPc applied on the cathode surface on power density as a function of current density
Variation of output voltage of an MFC with C-CoOx-CoPc cathode under 1 k external load for a long term operation

## Slide 43
RSC Advances, 2014, 4, 23790-23796
flower-like CuInS2 (CIS)
maximum power density = 0.108 mW cm-2
current density = 0.62 mA cm-2

## Slide 44
Energy & Environmental Science, 2014, 7, 3033-3039
maximum power density = 71 mW m-2
Hydrogen production rate= 7.5 umol h-1 cm-2
MoS3 modified p-type Si nanowire photocathode

## Slide 45
Energy & Fuels, 2010, 24, 1184–1190
Rutile-coated cathode
maximum power density (light irradiation)= 12.03 W m-3
maximum power density (dark condition)= 7.64 W m-3

## Slide 46
RSC Advances, 2015, 5, 82276-82281
maximum current density = 0.68 A m-2
Hydrogen production rate= 1.35 mL h-1

## Slide 47
Energy Technology, 2016, 4, 1–4
TiO2 photoanode
MFC
power density = 987 mW m-2
current density = 5.39 A m-2
PEC
power density = 257 mW m-2
current density = 1.93 A m-2
HPMFC
power density = 1645 mW m-2
current density = 8.84 A m-2

## Slide 48
Chemical Science, 2015, 6, 6799–6805
maximum power density = 1196 mW m-2

## Slide 49
ACS NANO, 2013, 10, 8728–8735
MFC
maximum power = 50 mW
current = 0.3 mA
PEC
Hydrogen production rate= 0.16 m3/m3/d