## Slide 1: Artificial Photosynthesis: From Molecular Catalysts for Light-driven Water Splitting to Photoelectrochemical Cells
Photochemistry and Photobiology, 2011, 87: 946–964

## Slide 2
Three steps of photosynthesis
Light-harvesting and local charge separation
Spatial charge separation
Multielectronic redox catalysis

## Slide 3: Molecular light-harvesting arrays
Photon energy is directionally transferred to a final acceptor
Dyad and triad models mimicking spatial charge separation
D: donor
P: photosensitizer
A: acceptor

## Slide 4
Multielectron photocatalysis
Sunlight-driven water splitting with sacrificial electron acceptor and donor

## Slide 5: Molecular catalytic systems for visible light-driven H2 evolution
Aim : develop noble metal-free molecular catalysts for light-driven H2 production
Pt group metals are excellent for H2 production but has limited supply and is of high cost
New photocatalysts based on earth-abundant first-row transition metals
Insight from structures of hydrogenase (H2ase)

## Slide 6: Homogeneous photocatalytic H2-evolving systems and photocatalytic bioconstructs based on hydrogenases
MBH : membrane-bound hydrogenase
PsaE : extrinsic subunit
PMS : N-methylphenazonium methyl sulfate, soluble electron carrier
lmax = 700 nm, iph = 85 nA/cm2
30% was H2
1) PSI-membrane-bound hydrogenase

## Slide 7
H2ase attached to PSI via dithiol
[4Fe-4S] cluster of C13G mutant of PSI PsaC subunit to distal [4Fe-4S] cluster of C97G mutant of [FeFe]-H2ase
Use ascorbate and PMS as sacrificial electron donor
Maintained stability for more than 2 months in the absence of O2
2) PSI-[FeFe]-hydrogenase

## Slide 8
3) [NiFeSe]-hydrogenase – TiO2 nanocrystalline thin film
Light is sensitized by Ru(bpy)32+
Use a sacrificial electron donor
Photoinstability was found

## Slide 9
Synthetic multicomponent photocatalytic H2-evolving systems
Two families of efficient catalysts
  Diiron mimics of the active site of [FeFe] hydrogenases
  Bioinspired cobalt complexes
Molecular photosensitizers
Ruthenium-based photosensitizers as light-harvesting units are most common

## Slide 10
Upon light absorption
  1 e- transition : d (metal)  p* (diimine ligand)
  Spin state : singlet (S=0)  triplet (S=1) by intersystem crossing due to spin-orbit coupling  3MLCT  Ru(III)L(-1)
PS* both as a strong reductant and a strong oxidant
  E(PS+/PS*) = -0.86 V
  E(PS*/PS-) = 0.84 V

## Slide 11
Other metal-diimine photosensitizers

## Slide 12
Other organic photosensitizers-a major breakthrough
Xanthene derivatives
Fluorescein : not a good photosensitizer
Heavy atoms (Br, I) facilitate inter-system crossing

## Slide 13
Diiron-based catalysts
Sacrificial donor
-ascorbic acid
photosensitizer
catalyst
TON = 86
TON = 200
Inorg. Chem. 2008, 47, 2805–2810.
Chemistry A European Journal 2010, 16, 60–63.

## Slide 14
Cobaloxime and cobalt diimine-dioxime catalysts
cobalt diimine–dioxime catalysts
cobaloxime catalysts

## Slide 15
Mechanistic issues
Initiation : absorption of a photon by photosentization. PS  PS*
Oxidative quenching or reductive quenching
Oxidative quenching
  PS* + Cat  PS+ + Cat-
  D + PS+  D+. + PS
  2Cat- + 2H+  2Cat + H2
Reductive quenching
  D + PS*  D+. + PS-
  PS- + Cat  PS + Cat-
  2Cat- + 2H+  2Cat + H2

## Slide 16
Sacrificial electron donors
-triethanolamine, TEOA
-triethylamine, TEA
Decomposition mechanism of TEA (R=H) and TEOA (R=OH) generating one electron (dark process)
The solution pH is important
  No H2 production at pH < 6-8, or above > 12-13
Solvent effects are to be considered

## Slide 17
Supramolecular photocatalysts
Single-component photocatalysts by supramolecular assembly or by covalent linking
photosensitizer
catalyst
photosensitizer
catalyst
TON : 103 for 11a
TON : 210 for 14

## Slide 18
Using a TiO2 nanoparticles
TON = 53
Supramolecular cobalt-based assemblies are more active than the corresponding multicomponent systems.

## Slide 19
Light-driven homogeneous water oxidation
Much insight from oxygen evolving center (OEC) of PSII – Mn4Ca
Photocatalytic bioconstructs based on PSII
Engineering PSII
Photocurrent = 45 mA/cm2
Osmium redox polymer acts as an electron acceptor
No sacrificial electron donors are needed

## Slide 20
Synthetic multicomponent photocatalytic oxygen-evolving systems
Mono- and dinuclear ruthenium-based photocatalytic systems
TON = 50 O2
370
580

## Slide 21
Photoelectrochemical device for water splitting
Voltage bias was applied
Three-component system: photosensitizer, catalyst, sacrificial electron acceptor
Sacrificial electron acceptor: [Co(NH3)5Cl]22+, S2O82-

## Slide 22
Ruthenium and cobalt-based polyoxometallates
Inorganic catalysts: more stable
Example: tungstosilicate, [RuIV4(O)4(m-OH)2(H2O)4(g-SiW10O36)2]10- catalyzes H2O by CeIV
TON = 385, yield 90%

## Slide 23
Bioinspired manganese-based photocatalytic systems
Mimicking OEC
–Dinuclear Mn(III) complexes with terpyridine or carboxylate-based ligands
-Cubane clusters
Issues to be addressed
  Stability of photosensitizers under highly oxidizing conditions
  Stability of catalysts to be systematically investigated
  Better understanding of mechanism of light-induced processes

## Slide 24
Perspectives
Challenge : developing a fully molecular-based device for H2 and O2 evolution system for water splitting
A fully homogeneous system where both H2 and O2 are evolved in one compartment
Drawback: explosive H2-O2 mixture, H2 has to be purified.

## Slide 25
Photoelectrochemical system
  Photoanode: water oxidation
  Photocathode: proton reduction

## Slide 26
Water splitting systems using semiconductors and metals
Semiconductor : photosensitizer
Metal : catalyst
6.3%
12.4%

## Slide 27
Issues to consider for molecular photocatalytic systems to be used
Catalysts for H2 and O2 evolution should work under the same operating conditions and tolerate the presence of H2 and O2.
Thermodynamic consideration
  Device A : PS* is first oxidatively quenched by H2-evolving catalyst  use TiO2 particle. TiO2 oxidatively quench PS* and dye injects an electron into the CB of TiO2, which can deliver it to a H2-evolving catalyst.
Fine control of the kinetics of the electron transfer steps.
  -Mimics of antennae effect
  -unidirectional electron transfer
  -Formation of long-lived charge separation states
   To be integrated in bioinspired photoelectrochemical cells