## Slide 1
Photo-sensitization by Light-Harvesting Complex (LHC) as a photocurrent generation unit

## Slide 2
Dye sensitization
An approach to better utilization of longer wavelength light
A thin layer of dye, D, is coated on the semiconductor
Eg > D
Eg
CB
VB
HOMO
LUMO
D
D  D+ + e-
e- is delivered to CB.
D+ + R  D + O
O + e-  R at the counter electrode

## Slide 3
Immobilization and Photocurrent Activity of a Light-Harvesting Antenna Complex II, LHCII, Isolated from a Plant on Electrodes
ACS Macro Lett. 2012, 1, 296−299

## Slide 4
Introduction
In this paper, LHCII was successfully immobilized on an ITO electrode with APS or with APS dot patterning and on a TiO2 electrode.
Immobilization of LHCII onto an ITO modified with APS by electrostatic attraction
APS: 3-aminopropyltriethoxysilane
Stromal side of LHCII – negatively charged, amine surface – positively charged

## Slide 5
Identification of immobilized-LHC Ⅱ on APS-ITO electrode.
Chlorophyll-a : 435 nm and 674 nm
Chlorophyll-b : 472 nm and 651 nm
The absorption spectrum of LHCII on APS-ITO was largely consistent with the spectrum in aqueous solution, indicating that the pigment complexes in LHCII were successfully assembled on the electrode without denaturation.
Solid : after immobilization
Dotted : in solution
Notes: Figure 1a shows the absorption spectra of LHCII isolated from spinach and after immobilization on an APS-ITO electrode.

## Slide 6
Identification of immobilized-LHC Ⅱ on APS-ITO electrode.
No fluorescence of LHCII was observed on the SiOH domain that is not modified with APS.
Notes: Figure 1b,c shows the fluorescence images of LHCII on the electrode with APS dot patterns and the fluorescence intensity profile.

## Slide 7
Cationic surface (Electrode)
Anionic stromal side (LHC II)
Anionic stromal side
Identification of immobilized-LHC Ⅱ on APS-ITO electrode.
Electrostatic interactions
COO-
Notes: This selective attachment indicates that the assembly of LHCII onto the APS-ITO electrode was affected by electrostatic interactions
between the cationic surface of the electrode and the anionic stromal side of the LHCII polypeptide which includes anionic residues
such as aspartic acid or glutamic acid in the sequence of the protein.

## Slide 8
Cathodic photocurrents were observed, implying that photoinduced electron transfer from LHCII to MV2+ occurred more efficiently than the back electron transfer to the electrode.
Photocurrent measurement of immobilized-LHC Ⅱ on APS-ITO electrode.
670 nm (solid line)
465 nm (dotted line)
Notes: Figure 2. (a) Photocurrent response of LHCII assembled on an APS-ITO electrode in buffer solution when illuminated at 670 nm (solid line) and 465 nm (dotted line).

## Slide 9
Efficient photocurrent responses were observed upon illumination around 470 and 670 nm corresponding to chlorophyll-a/b in the complex, and this response was particularly efficient for chlorophyll-a.
The energy absorbed by the stromal chlorophylls is quickly focused on chlorophyll-a clusters such as five Chl a and is further transmitted to the neighboring LHCs or reaction centers.
Photocurrent measurement of immobilized-LHC Ⅱ on APS-ITO electrode.
Notes: Figure 2b shows the action spectra expanded from the point where the largest negative current was obtained as shown in Figure 2a, in conjunction with the absorption
spectrum of the LHCII assembled onto APS-ITO.

## Slide 10
The absorption spectrum of LHCII on the TiO2 nanostructured film was approximately consistent with the spectrum in aqueous solution, indicating that the pigment complexes in the LHCII system assembled on the TiO2 film were stable and the native state was preserved.
Photocurrent measurement of immobilized-LHC Ⅱ on TIO2 electrode.
Notes: Figure 2c shows the absorption and photocurrent response spectra of the LHCII assembled on TiO2 in the iodide / tri-iodide redox system of an
ionic liquid based electrolyte.
Figure 2d shows the I−V characteristics of the dye-sensitized solar cells (DSSC) for LHCII (Scheme 1d).
LHCII was assembled onto a TiO2 nanostructured film.
It is likely that assembly of LHCII on the electrode was facilitated by the many carboxyl residues such as aspartic acid or glutamic acid, contained in the protein
sequence of LHCII, which binds easily to the surface of TiO2.

## Slide 11
Comparison of immobilized-LHC Ⅱ on APS-ITO and TIO2 electrode.
Remarkable enhancement of the photocurrent was observed when measured in the iodide/tri-iodide redox system of an ionic liquid based electrolyte on the TiO2 electrode in comparison to that on the ITO electrode.

## Slide 12
Conclusion.
The photocurrent action spectrum was reasonably consistent with the absorption spectrum of LHCII, indicating chlorophyll-a clusters on the stromal chlorophylls play an important role on the photocurrent activity.
Conversion efficiency of the photocurrent measured in the iodide/tri-iodide redox system of an ionic liquid based electrolyte on the TiO2 electrode was significantly enhanced in comparison to that on the APS-ITO electrode.
These results indicate that LHCII acts as an effective photosensitizer material with a wide absorption band, and it is a potential candidate for photoenergy conversion materials.

## Slide 13
Enhanced photocurrent production by bio-dyes of photosynthetic macromolecules on designed TiO2 film
Daoyong Yu1,2, Mengfei Wang2, Guoliang Zhu2, Baosheng Ge1,2, Shuang Liu2 & Fang Huang1,2
Scientific Reports, 5, 9375 (2015)
Notes: I have chosen this paper.
This paper title is "Enhanced photocurrent production by bio-dyes of photosynthetic macromolecules on designed TiO2 film".
This paper designed three types of TiO2 films on FTO glass for the sensitization of Photosystem I (PSI) and light-harvesting complex II (LHCII), and explored the effects of pigment-protein complex on the performance of biohybrid photovoltaic cells.

## Slide 14
Introduction
Photosystem Ⅰ(PSⅠ) and Light-harvesting complex II(LHCII)
PSⅠ and LHCII existed in thylakoid membrane of photosynthetic bacteria and plants and are a viable alternative natural photosensitizers.
The photons of light is collected by light-harvesting antenna complexes of PSⅠ and LHCII with internal quantum yield near 100%.
Dye Sensitized Solar Sell (DSSC)
< Photosystem Ⅰ>
< Light-harvesting complex II >

## Slide 15
Introduction
Adv. Funct. Mater. 2014, 24, 7467–7477
Phys. Chem. Chem. Phys., 2014, 16, 20856--20865
< PSⅠ>
< LHC II >

## Slide 16
Figure 1 Top view photos of TiO2 electrodes of (a) 6 type, (b) 6+1 type, and (c) 1+1 type, and schematic presentation of electrodes of (d) 6 type, (e) 6+1 type, and (f) 1+1 type.
Figure 2 Top view SEM images of nanocrystalline TiO2 electrodes. (a) 6 type; (b) 6+1 type; (c) 1+1 type. Inner images’ width 1 mm.
6 type TiO2 electrode was composed of 6 layers of ~2 μm thick transparent layer (mesoporous TiO2 : ~20 nm particle size).
6+1 type TiO2 electrode was composed of ~2 μm scattering layer (porous layer : ~200 nm particle size) on top of the 6 type TiO2 electrode.
1+1 type TiO2 electrode was composed of a ~2 μm scattering layer (porous layer : ~200 nm particle size) on top of ~2 μm thick transparent layer (mesoporous TiO2 : ~20 nm particle size).
6 type
6+1 type
1+1 type
Experimental section
Notes: In this paper, three types of TiO2 electrodes were designed.
6 type TiO2 electrode was composed of 6 layers of ~2 μm thick transparent layer (mesoporous TiO2 : ~20 nm particle size).
6+1 type TiO2 electrode was composed of ~2 μm scattering layer (porous layer : ~200 nm particle size) on top of the 6 type TiO2 electrode.
1+1 type TiO2 electrode was composed of a ~2 μm scattering layer (porous layer : ~200 nm particle size) on top of ~2 μm thick transparent layer (mesoporous TiO2 : ~20 nm particle size).

## Slide 17
Experimental section
Figure S1 Dimensional size of PSI (PDB ID: 1JB0) and LHCII (PDB ID: 1RWT). (a) PSI monomer. (b) Lumenal side of trimeric PSI complex constructed from 1JB0. (c) LHCII trimer. Marked sizes are measured by PyMOL.
The assembly of PSI or LHCII on the electrode is facilitated by the many carboxyl residues such as aspartic (D) or glutamic acid (E), in the protein sequences of PSI or LHCII, which bind easily to the surface of TiO2.
< PSI >
< LHCII >
H. Hug et al. / Applied Energy 115 (2014) 216–225
Stromal side
Notes: This paper used two photosynthetic protein complexes, PSI and LHCII as bio-sensitizer.
The stromal side of PSI or LHCII has more carboxyl groups on the surface and it will tend to be preferentially fixed on TiO2 surface.
The possible binding modes of carboxyl group to TiO2 include coordinate covalent, carboxylate, and hydrogen bonds.

## Slide 18
The PSI trimer solubilized in DDM solution is not very stable and some trimers dissociate to monomers.
Additionally, the high concentration(400 μg Chl/mL) of PSI trimmer is stable than the low concentration(80 μg Chl/mL).
Figure 4 Fluorescence spectra of (a) PSI solutions and PSI-TiO2 electrodes, (b) LHCII solutions and LHCII-TiO2 electrodes, normalized at maxima.
Figure 3 Sucrose density gradient centrifugation of DDM-solubilized PSI after incubation of 30 min and 96 h respectively, performed by the method described in Ref. 42.
n-Dodecyl β-D-maltoside (DDM)
t-Octylphenoxypolyethoxyethanol (Triton X-100)
Results
Notes: In this paper, surfactant DDM instead of Triton X-100 was used to keep PSI or LHCII, and to inhibit the formation of multilayer on the TiO2 surface.
As you can see in figure 3 and 4a, the PSI trimer solubilized in DDM solution is not very stable and some trimers dissociate to monomers.
On the other hand, the LHCII trimer solubilized in DDM solution is stable.

## Slide 19
Figure 5 (a) Top view photos of PSI-sensitized TiO2 electrodes of 1+1, 6+1 and 6 types. (b) Top view photos of LHCII-sensitized TiO2 electrodes of 1+1, 6+1 and 6 types. Adsorption models of PSI@TiO2 electrodes of (c) 6, (d) 6+1, and (e) 1+1 types. Adsorption models of LHCII@TiO2 electrodes of (f) 6, (g) 6+1, and (h) 1+1 types.
Results
PSI and LHCII are macromolecules, and the size screening effect of the mesopore in TiO2 layer controls the adsorption depth of these macromolecular bio-dyes.
In the case of PSI, the PSI can be fixed not only on the surface but also in the inner, but can’t diffuse into the inner deeper mesopore of the transparent TiO2 layer.
However, the LHCII can be fixed not only on the surface but also in the inner mesopores of both the scattering layer and the transparent TiO2 layer.
( Monomer diameters: ~13 nm, Trimer diameters: ~ 22 nm )
( Trimer diameters: ~ 6 nm )
Notes: The pigments of PSI and LHCII on TiO2 electrode are non-covalent binding, and can be easily extracted by a mixed solvent of 80% acetone.
Table 1 is the pigments concentration of PSI or LHCII on TiO2 electrode.
Comparing the 6+1 with the 6 type electrode, addition of the scattering layer (porous layer : ~200 nm particle size) helps to increase the adsorbance of PSI and LHCII.
In the case of PSI, the PS1 can be fixed not only on the surface but also in the inner, but cannot diffuse into the inner deeper mesopore of the transparent TiO2 layer.
However, the LHCII can be fixed not only on the surface but also in the inner mesopores of both the scattering layer and the transparent TiO2 layer.
These results indicate that enhancing the thickness of the transparent layer can increase the absorbance of LHCII.

## Slide 20
Results
Figure 6 The current-voltage characteristics measured under AM 1.5 G solar irradiance (100 mW cm-2 photon flux) for (a) PSI-sensitized, (b) LHCII-sensitized, and (c) blank solar cells with different TiO2 electrodes.
In the case of PSI-SSC, the adsorbances of PSI on the 6+1 type and 1+1 type electrodes are similar, but resistance of the 6+1 type is higher than the 1+1 type.
In the case of LHCII-SSC, the adsorption of LHCII on the 6+1 type is deeper than the 1+1 type, and the addition of the scattering layer increases the light absorption by LHCII in the transparent layer.
These results indicate that the adsorbance of bio-dye and the resistance of equivalent circuit for sensitized solar cell (SSC) has an important effect on the performance.
A 6+1 type
A 6 type
A 1+1 type
=
>
Rs 1+1 type
Rs 6+1 type
Rs 6 type
=
<
A 6+1 type
A 6 type
A 1+1 type
<
>
Rs 1+1 type
Rs 6+1 type
Rs 6 type
=
<
Notes: In the case of PSI-SSC, the adsorbances of PSI on the 6+1 type and 1+1 type electrodes are similar, but resistance of the 6+1 type is higher than the 1+1 type.
As you can see in figure 6a, the efficiency of 1+1 type (PSI-SSC) is better than the 6+1 type (PSI-SSC).
In the case of LHCII-SSC, the adsorption of LHCII on the 6+1 type is deeper than the 1+1 type, and the addition of the scattering layer increases the light absorption by LHCII in the transparent layer.
As you can see in figure 6b, the efficiency of 6+1 type (LHCII-SSC) is better than the 1+1 type (LHCII-SSC).
These results indicate that the adsorbance of bio-dye and the resistance of equivalent circuit for sensitized solar cell (SSC) has an important effect on the performance.

## Slide 21
Results
Figure 7 Incident photocurrent conversion efficiencies (IPCE) as a function of wavelength. (a) PSI-SSC, (b) LHCII-SSC with photoanodes possessing different layers of TiO2 on conductive FTO glass.
The IPCE spectra of PSI-SSC or LHCII-SSC is similar to the absorption spectrum in solution.
These IPCE results indicate that LHCII or PSI can be excited by the captured photons and inject electrons into the conducting band of the TiO2 film.
Notes: As you can see in figure 7, the IPCE spectra of PSI-SSC or LHCII-SSC is similar to the absorption spectrum in solution.
These IPCE results indicate that LHCII or PSI can be excited by the captured photons and inject electrons into the conducting band of the TiO2 film.

## Slide 22
Results
Figure 8 Simple energy level diagram for bio-sensitized solar cell. The potentials are shown for (a) PSI-SSC and (b) LHCII-SSC. The primary free energy losses are associated with electron injection from the excited sensitizer into the TiO2 conduction band (CB) and regeneration of the dye by the redox couple.
VOC = 0.59 V
VOC = 0.6 V
Notes: The open circuit voltage of PSI-SSC and LHCII-SSC is 0.59 and 0.60 V respectively, which is approximately indicated by the splitting between the TiO2 Fermi level and the chemical potential of the redox electrolyte.
The PSI-SSC has the efficient energy transfer in the antenna system and the high efficiency of charge regeneration than the LHCII-SSC.
Therefore, the overall performance of PSI-SSC is higher than the LHCII-SSC.

## Slide 23
Conclusion.
PSI and LHCII exist in thylakoid membrane of photosynthetic bacteria and plants and are a viable alternative natural photosensitizers.
The morphology of TiO2 film has a large effect on both the adsorbance and the depth of bio-dye adsorption.
PSI shows its merit of high efficiency for captured energy transfer, charge separation and transfer in the electron transfer chain (ETC), and electron injection from FB to the TiO2 conducting band.